## Slide 1
High temperature Exchanger Remaining life assessment
Author: Shaikh Noor Uddin
(SABIC-Petrokemya)

## Slide 2: Contents
Introduction
  Background
  Process description
  Challenges
Assessment summary
  Exchanger details
  Brief History
  Study basis & assumptions
  Level-1 & level-2 applicability
  Assessment detail
  Conclusion & forward plan
  References

## Slide 3: introduction
High temperature Exchanger remaining life assessment
  Background
  Process description
  Challenges

## Slide 4: Background
This exchanger commissioned in our plant around 2000, which operates at elevated temperature & installed inside reactor.
Concerns were raised over its integrity & reliability, due to high temperature degradation. It was identified to perform technical assessment for all components of exchanger, considering high temperature affects.
Results would be used to develop inspection requirement, formulate replacement strategies & identify remaining life.

## Slide 5: Process Description
Reactor Effluent
Hydrocarbon
Vapor
Heat
Exchangers
Heater
Steam
1st stage Reactors
Symbolic Process block Flow
2nd stage Reactors
Steam interchange exchanger
Coil# B
Coil# A
600~800oC
500~600oC
600~700oC
400~500oC
Around 600~800oC super-heated steam from Heater reheats 1st stage reactor effluent on shell side of Steam Interchange exchanger located inside 2nd Stage reactor.
Steam returns to Heater around 500~600oC & is heated in Coil B to 600~700oC (approx.).
From Coil B, heated steam enters at bottom of 1st Stage reactor, where it mixes with hydrocarbon around 400~500oC from heat exchanger.
Mixture flows upward into inner cylinder of reactor, then radically through catalyst bed into outer annular space & upward to exit nozzle.
1st stage reactor Effluent enters in 2nd reactor &undergoes further processing, later routed to waste heater exchanger.

## Slide 6: Challenges
Exchanger arrangement (located inside reactor)
Bottom tube-sheet accessibility (located in 2nd level of confined space & very limited access)
Tube cleaning (i.e. dry & wet Tube cleaning never performed due to its complex arrangement)
1st stage
Reactor
Effluent
Expansion
Bellow
Expansion
Bellow
MW
IMW
IMW``
MH
MH
MW
MW
Steam inlet
2nd stage Reactor
Steam Outlet
Waste heat
exchanger
Exchanger
Catalyst
screen
Screen

## Slide 7: assessment summary
High temperature Exchanger remaining life assessment
  Exchanger details
  Brief History
  Study basis & assumptions
  Level-1 & level-2 applicability
  Assessment details

## Slide 8: Exchanger specification
Component Description | Design Pressure | Design Temp. | Material
Inlet Nozzle | 100~200 Kpa | 850~900oC | SB409 / Alloy 800HT
Outlet Nozzle | 100~200 Kpa | 550~600oC | SA204-TP304H
Shell | 100~200 Kpa | 650~700oC | SA204-TP304H
Tubes | 100~200 Kpa | 650~ 700oC | SA249-TP304H
Steam inlet
Steam Outlet
Exchanger Arrangement
Expansion Bellow
Top Tube sheet
Bottom Tube sheet
Inlet nozzle pipe
Outlet nozzle pipe
Shell
Tubes
Hydrocarbon inlet
Hydrocarbon inlet

## Slide 9: Why study is needed?
High temperature materials are specially selected in design to exhibits strength under continuous high temperature exposure.
  SS304H (up to 815 oC & creep starts at 515 oC)
  Alloy 800HT (around 900 oC & creep starts at 565 oC)
  (As per API & ASME standard)
Although, these materials are design to sustain high temperature loads, but material will still degrade over time under continuous exposure to high temperature & stress. The following damage mechanisms are applicable to high temperature material degradation:
  High temperature creep (this study is limited for this damage mechanism)
  Sigma Phase embrittlement (No destructive examination performed, hence, no assessment)

## Slide 10: Brief History
2010
No finding in Visual & Weld DPT
2012
No finding in Visual & Weld DPT
No finding in tubes Borescope
No ECT performed due to tube fouling
2014
No finding in Visual & Weld DPT
No finding in tubes Borescope
Tube pulling not attempted successfully
No ECT performed due to tube fouling
2016
No finding in Visual & Weld DPT
No finding in tubes Borescope
Tube pulling not attempted successfully
No ECT performed due to tube fouling
2021
Awaited
2018
No finding in Visual & Weld DPT
No finding in tubes Borescope
No ECT performed due to tube fouling
No finding in accessible location replica
Hardness found within limits
Summary:
Five inspection techniques utilized (i.e. Visual, DPT, Borescope, hardness & Replica only on accessible location).
ECT & tube sampling never conducted, hence real tube condition is not known.

## Slide 11: Brief History
Maintenance
Historically, no maintenance performed
Operation
No temperature excursions from design limits

## Slide 12: Study basis & assumption
Physical sign
No cracks reported in exchanger shell, tube sheet & tubes
No geometric abnormality signs reported
No pitting & low thickness losses reported
No dents, bulge and mis-alignment reported
Material degradation
Hardness test found within acceptable limit
Replica did not show metal degradation signs
Operation upsets
equipment PI- trends shows operating temperature & pressure are within design limits
API 579 chapter 10 level -1 & level-2 assessment tools used for high temperature & exchanger remaining life study using Larson Miller approach.
As per available inspection, operation & maintenance history, following are study assumption & basis.

## Slide 13: Level 1 assessments
Comparison with specified t-T-s limits & a simplified creep damage calculation for components under operating conditions.
t = Time
Referenced case is around 20 years old
T = Temperature
Operating case is within design case (study performed on design temperature)
S = Stress
Operating stress calculated using API-579 Annex 2 C

## Slide 14: Assessment applicability
    Level-1 is applicable, if below condition meet:
Original design are in accordance with code.
Component has not been subject to fire.
Material exceeds minimum hardness & carbon content requirement.
The component does not contain
  Local Thin Area (LTA), groove, pitting
  Blisters
  Weld misalignment
  Dents or bulges, out of roundness
  Cracks
  Graphitization, sigma phase
Level-1 validation
    Level-2 is applicable, if below condition meet:
Original design are in accordance with code.
No cyclic loading.
The component does not contain any of the flaws listed in level-1.
Level-2 validation

## Slide 15: Level -1 assessment summary
Component | Temperature | Pressure | Time | Material | Diameter | Stress (A) | Screening curve | Assessment result
Inlet pipe | 850~900oC | 100~200 Kpa | Approx. 20 years (i.e. 175,000 hour) | SB409 / Alloy 800HT | 1700mm | 6.0 Mpa | Refer API-579 Figure 10.25 | Creep Damage < 25%, So, Level-1 criteria satisfied, RLA > 250,000 hours
Outlet pipe | 550~600oC | 100~200 Kpa |  | SA204-TP304H | 1050mm | 5.5 Mpa | Refer API-579 Figure 10.16 | 
Tube | 650~700oC | 100~200 Kpa |  | SA249-TP304H | 50mm | 2 Mpa |  | 
Shell | 650~700oC | 100~200 Kpa |  | SA204-TP304H | 5000mm | 22.5 Mpa |  | Damage >25%, & RLA < 175,000 hours So, Level-2 study is required
(A) Stress is calculation using Annex 2C specified formulae

## Slide 16: Level -2 assessment summary
Component | Effective Stress (1) | Larson Miller parameter (2) | Creep Damage (3) | Remaining life (4) | Assessment result
Shell | 18 Mpa | 15.5 | 0.155 | <100 years | Creep Damage < 1, so, Level-2 is accepted
(1) Calculated using API 579 Equation 10.12
(2) Taken from API 579 table 10B.4M
(3) Calculated using API 579 Equation 10.26
(4) Calculated using API 579 Equation 10.22

## Slide 17: Conclusion & forward plan
High temperature Exchanger remaining life assessment

## Slide 18: Conclusion & forward plan
Extend inspection
- Explore tube cleaning option that allow tube NDT inspection.
- Conduct borescope inspection for exchanger outside shell condition, its associate support bracket.
- Evaluate possibility of performing hydro-test.
Execution feasibility
- Explore option for designing of temporary platform for accessing bottom tube sheet.
Forward plan
Conclusion
Studied exchanger components creep life are more than 25 years, hence, exchanger is recommended for continue operation without immediate replacement.
Disclaimer: This RLA do not consider any localize flaw & utilized limited history & need to re-visit with recent inspeciton finding.

## Slide 19: References
ASME International & American Petroleum Institute, “API 579-1/ASME FFS-1 - Fitness-For-Service,” 2016.
American Petroleum Institute, “API 579-2/ASME FFS-2 2009- - Fitness-For-Service Example Problem Manual,” 2009.
Signal FFS software from Quest Integrity ™ Group.

## Slide 20
Thank You