## Slide 1
"Navigating the Unseen”
Corrosion/Erosion in Refining ,petrochemical & Chemical industries
Presented By: Abhishek Agrawal
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES

## Slide 2
Statement of problem
General assembly drawing
History
Retubing Activity
Unique failure
What went wrong
Code information of strength weld
Lesson Learned
INDEX

## Slide 3
Statement of problem
Detection ,Managing and Solution of unique failure in static equipment is a great challenge for inspection and NDT personnels.
Unique failure have been predominantly linked with harsh operating condition, non availability of qualitative NDE methodology & unclear guiding in code & Standard for QA/QC.
Inadequate maintenance strategies, Inappropriate Material of construction of equipment leads to unplanned shutdowns and costly repairs.

## Slide 4: General Assembly drawing
BFW Inlet
P= 71.38 Kg/cm2
T= 105 C
BFW Outlet
P= 71.38 Kg/cm2
T= 165 C
Condensate Outlet
P= 11.2 Kg/cm2
T= 127 C
Condensate Inlet
P= 11.2 Kg/cm2
T= 188 C

## Slide 5: History
SECT test revealed top 06 rows had suffered with severe erosion damage
Most defected tubes pulled & found damages were located specifically below the implement plate
Retubing decision postponed due to TAM frequency
Top 03 rows were plugged followed with HT and boxed up

## Slide 6: Retubing activity
Impingement plate condition was found satisfactory
Pressure boundary inspected
217 mm
Tube sheet thickness

## Slide 7: Timeline (06 Month after Re tubing)
Increased BFW consumption
Impact noticed sustainability data
within 03 month
Suspected leakage from BFW preheater
Planned for Emergency Shutdown and opened heat Exchanger

## Slide 8: Unique failure
Hole observed on tube sheet in one of the preheater
50~70% Tube sheet thickness eroded
Approximate 30 mm diameter through hole in one location

## Slide 9: Tubes condition
Tubes near by hole were severely thinned
Broken tubes around the hole
Cross section area of broken tubes around the hole

## Slide 10: What went wrong
Tube sheet
Tube
13 mm
Expansion area 201 mm
3 mm
Shell side
Tube side

## Slide 11: Code information of strength weld

## Slide 12: Lesson Learned
Only full defect free TTSJ shall be acceptable to avoid such issues industry .
It is advisable to perform Pneumatic test after first expansion during retubing.
DP Examination to be performed after first pass TTSJ weld joint .
Stringent inspection scope to be defined ,in case of hiring the TPI/ASME inspectors .
No any specific guideline available in code/standard for QA of TTSJ .
No any quantitative NDE available to verify TTSJ except VI,DPE, PT & HT

## Slide 13
Abhishek Agrawal
THANK YOU
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES
+966-594326457
Agrawalay@sabic.com