## Slide 1
Jubcor Presentation
Presented By: Dr. Azhar Alhasawi
And Dr. Ihsan Ul haq Toor
YOUR LOGO
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES
Recent advances in understanding MIC and prevention strategies-A review
*R&D Principal Chemist, Halliburton
*Associate Professor, KFUPM

## Slide 2
Outline:
The definition of MIC.
The cost of MIC.
Corrosion causing microorganism/ Microbial corrosion in metals.
Mechanism of biocorrosion: Ennoblement/role of biofilms.
Type of alloys affected by MIC.
Biocorrosion control strategies.
Monitoring Techniques .
The gaps in MIC research.
Conclusions and future perspectives.

## Slide 3
MIC Historical Perspective
Lavanya M (2021). J Bio- Tribo-Corros 7(3):1–9.

## Slide 4
Chart: MIC Publication Numbers
MIC Pulication Numbers | 488 | 537 | 737 | 896 | 925
Economic impact of MIC
2020

## Slide 5
MIC Considerations in different industries

## Slide 6
MIC types and corrosion mechanisms

## Slide 7
Microbe name | Type | Trait | Effect | References
Sulfide reducers Desulvovibrio sp. Desulfomonas sp. | Anaerobic | Use H2 to reduce SO42− to S2−: precipitation of H2S and FeS | Cathodic depolarization by hydrogen uptake, anodic depolarization by corrosive iron sulfides | Enning et al., 2012; Rao et al., 2000; Venzlaff et al., 2013; Wikieł et al., 2014
Iron oxidizers/manganese oxidizers Gallionella sp. Leptothrix sp. Mariprofundus sp. | Aerobic | Fe2+ to Fe3+ and Mn2+ to Mn3+: Iron oxide and manganese dioxide formation | Deposition of cathodically reactive ferric and manganic oxides | Lee et al., 2013; McBeth et al., 2011; Rao et al., 2000; Linhardt, 2010
Iron reducers Pseudomonas sp. Shewanella sp. Geothermobacter sp. | Aerobic | Reduce Fe3+ to Fe2+, manganese or iron oxide reduction | Reduction of iron and manganese oxides | Lee et al., 2013; Rao et al., 2000
Sulfide oxidizers Thiobacillus sp. | Aerobic | Oxidizes S2− and SO32− to H2SO4 | Acids corrode metal | Li et al., 2008
Acid producing bacteria and fungi Clostridium sp. Fusarium sp. Penicillium sp. Hormoconis sp. | Aerobic and anaerobic | Production acids, e.g., nitric acid, sulfuric acid, and organic acids | Dissolve iron, chelate copper, zinc and iron | Juzeliūnas et al., 2007; Little et al., 2001; Usher et al., 2014
Slime forming bacteria Clostridium sp. Bacillus sp. Desulfovibrio sp. Pseudomonas sp. | Aerobic and anaerobic | Production of extracellular polymeric substances (biofilm) | Exopolymers capable of binding metal ions | San et al., 2011; Stadler et al., 2008; Stadler et al., 2010
Nitrate reducing Halomonas titanicae | anaerobic | The extracellular electron transfer (EET) | Increasing the corrosion of two marine structural steels in an anaerobic seawater environment enriched with nutrients. | https://doi.org/10.1016/j.corsci.2023.111125 Lue et al., 2023
red-tide alga Phaeodactylum tricornutum and its symbiotic bacterium Bacillus altitudinis | anaerobic | Biofouling | The corrosion-biofouling-accelerated corrosion-deteriorated biofouling formed a vicious cycle. | https://doi.org/10.1016/j.jmst.2022.02.057 Dong et al., 2022
The microbes involved in corrosion process.

## Slide 8
Material/MIC interactions
Carbon steel
Biofilm morphologies on the surface of steel
S. Lu et al (2023). Corros. Sci
Costa. 2021. Microbial Corrosion in Titanium-Based Dental Implants: How Tiny Bacteria Can Create a Big Problem?

## Slide 9
Material/MIC interactions
Titanium
Corrosion mechanism in Ti materials ( Costa, 2021 )

## Slide 10
Environmental factors responsible for MIC

## Slide 11
Environmental factors responsible for MIC
Dake Xu., et al (2023). Nature Reviews Microbiology. 21 (11)

## Slide 12
MIC testing and monitoring
Micrbiology
Culture based methods
Plate counts
Microscopy
Light microscopy
Other methods
FTIR
ATR
Most probable number (MPN)
Test kits to enumerate MIC
2D or 3D optical tomography
Confocal laser microscopy
Electron microscopy
Atomic force microscopy
Scanning electron microscopy
DNA/RNA/ protein technique
Enzymatic methods
Metabolomics
XRD
EDX
surface profiling
Raman spectroscopy

## Slide 13
MIC prevention strategies
Control Measure
Biocide
Protective coating
UV treatment
Cathodic protection
Corrosion inhibitors

## Slide 14
MIC Monitoring
Weight loss
Electrical method
NDT techniques

## Slide 15
Alternative MIC Monitoring Techniques
Alternative method for MIC monitoring from (Puentes-Cala, 2022)

## Slide 16
MIC Inhibiting Agents
Jana et al. ( 2022)

## Slide 17
MIC Inhibiting Agents
Schematics of the formation of oil-containing graphene oxide microcapsules and the preparation of GOMCs/PU coatings. Juzeliūnas, et al. (2007).

## Slide 18
Simulation and data science tools (AI/ML)
Different type of models and their applicability to understand MIC at different scales. Deterministic models are highlighted in blue and non-deterministic models in red (Wolodko J., et al. NACE-2018-11398)
.

## Slide 19
Reach out.
THANK YOU
Azhar-444@outlook.com
0564876020
Calle Cualquiera 123, Cualquier Lugar
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES
YOUR LOGO
0558096194
ihsan@kfupm.edu.sa