## Slide 1
CORROSION BEHAVIOR OF 3D PRINTED
316 L STAINLESS STEEL IN CHLORIDE
AND HYDROCARBON ENVIRONMENTS
Presented By: Ibrahim Albalawi
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES

## Slide 2
Agenda
Introduction
What is additive manufacturing
Additive VS Convectional Manufacturing
SLMed 316L Stainless Steels Fabrication
Experimental Procedure and methodology
Results and discussion
Conclusions and recommendations
References

## Slide 3
Introduction
Corrosion is a major issue in the oil and gas industry. It results from the interaction of metal with the corrosive environment, which can lead to leaks, explosions, and other safety risks.
To overcome this challenge, oil and gas industries use high corrosion resistance material.
One of most common materials that are used is 316L Stainless steel.
This type of stainless steel can be fabricated by convectional manufacturing and additive manufacturing

## Slide 4
What is additive manufacturing
FIGURE 2: 3D printing types [2].
Additive manufacturing (AM) is a process by which computer-controlled machines build up objects from layers of material. This can be anything from toothpaste to airplane wings, and even prosthetic limbs for amputees.

## Slide 5
What is additive manufacturing
The selective laser melting technique (SLM), also known as direct metal laser melting (DMLM), is an advanced AM technique that uses a high-power laser to melt and fuse powdered metals.
FIGURE 3: The schematic of an SLM process [2].

## Slide 6
Additive VS Convectional Manufacturing
  Short fabrication time.
  AM enables manufacturers and industries to create complex structures.
  Reduce material waste.
  Eliminate indirect cost.
  faster prototyping and product development cycles.
  reduce the environmental impact of traditional manufacturing processes.
FIGURE 1 A comparison of traditional and additive manufacturing [1]
Advantages of Additive Manufacturing:
Notes:   Short fabrication time.
  AM enables manufacturers and industries to create complex structures.
  Reduce material waste.
  Eliminate indirect cost. such as transportation, storage cost, and reducing the need for large inventories.
  faster prototyping and product development cycles.
  reduce the environmental impact of traditional manufacturing processes.

## Slide 7
SLMed 316L Stainless Steels Fabrication
Where:
is the Laser power in W,
is the scanning speed in mm/s,
is the hatch spacing in mm,
is the Layer thickness in mm.
In SLM-based manufacturing, a high energy density may be employed to create materials with a density greater than 99.8%.
Each SLM process parameter can affect the material’s density.
Energy Density (Ed) Equation:
FIGURE 4 SLM 3D printing Process parameters [3]

## Slide 8
SLMed 316L Stainless Steels Fabrication
The rate of cooling and geometry of the melt container directly influences the microstructure and grain growth in the produced part.
Laser scan direction and energy density affect the microstructure and the relative density.
Impact the corrosion resistance of the SLM 3D printed material.
FIGURE 5 An illustration of melting and solidification of stainless steel in SLM [4]

## Slide 9
Effect the process parameters on the Microstructure
The physical and mechanical characteristics of SLM materials can be impacted by the SLM process parameters.
At the macroscale, the SLM process causes the creation of overlapping melt pools with a semicircular shape in the plane perpendicular to the direction of construction
Pores were can be caused by 3D printed materials in low energy density.
FIGURE 6 The microstructures of different samples, (a)-wrought, (b)-SLM XY 316 L stainless steel, and (c)- SLM XZ 316 L stainless steel[5]

## Slide 10
Effect the process parameters on the Microstructure
FIGURE 7 Microstructure image of 36 SLMed 316L specimens with blue line dot for almost compete melting energy density [6]
FIGURE 8 SLM process conditions Map with the theoretically calculated melting energy density [6]

## Slide 11
Experimental Procedure and Methodology
Materials
The 316L stainless steel has been selected for this work due to its important in oil and gas industry and less available research in industry environment.
Elements | C | Mn | Mo | S | P | O | Ni | Cr | Fe
SLMed | 0.03 | 2 | 2.25 | 0.01 | 0.025 | 0.05 | 13 | 17.1 | Bal.
Wrought | 0.03 | 2.2 | 2.3 | 0.03 | 0.05 | 0.05 | 11.2 | 17.5 | Bal.
Fabrication
The wrought samples was fabricated by using conventional casting methos and were bought from the local market. The SLMed 316L stainless steel samples were fabricated by using Selective Laser Melting (SLM).
FIGURE 9 Fabricated samples by SLM technique 20 x 20 x 4 mm.

## Slide 12
Experimental Procedure and Methodology
Fabrication
Sample Name | Laser power (W) | Scan speed (mm/s) | Layer thickness (mm) | Trace width (mm) | Energy density (J/mm3)
ED20 | 180 | 1270 | 0.045 | 0.15 | 21.0
ED30 | 180 | 800 | 0.045 | 0.15 | 33.3
ED30T | 180 | 800 | 0.045 | 0.15 | 33.3
ED40 | 180 | 650 | 0.045 | 0.15 | 41.0
W-316L | conventional manufacturing for 316L stainless steel - Wrought Sample of 316L |  |  |  | 
The samples were printed with different energy densities, as calculated by the formula below:
Where:
is the Laser power in W,
is the scanning speed in mm/s,
is the hatch spacing in mm,
is the Layer thickness in mm.

## Slide 13
Experimental Procedure and Methodology
Microstructure Characterizations
All samples were Grinded and polished and prepared as per ASTM G1.
To reveal the microstructure of samples, a solution having 3 parts nitric; 1-part HCL; 5 parts deionized water was used as an etchant.
The samples of wrought 316L stainless steel and SLMed 316L stainless steel were characterized using Optical Microscope (GX53 olympus) to obtain and evaluate the microstructure of all samples before corrosion test.
XRD was performed to analyze the characterizing crystalline materials and obtain more information about the structure, phases and crystallinity.

## Slide 14
Experimental Procedure and Methodology
Electrochemical Corrosion Test
All electrochemical experiments were conducted in 3.5% NaCl at room temperature with four pH values; pH-1, pH-3, pH5, and pH 7.5.
The pH values were controlled by adding HCl to the solution.
The corrosion analysis was carried out using:
    Linear Polarization Resistance (LPR),
    Potentiodynamic Polarization (PDP),
    open circuit potential (OCP),
    Electrochemical impedance spectroscopy (EIS)

## Slide 15
Experimental Procedure and Methodology
Immersion Corrosion Test
316L SLMed (ED30T) stainless steel and the 316L wrought samples were immersion in:
  3.5% NaCl
  crude oil (hydrocarbon)
Immersion duration: 14 days (336 h )
Test temperature: room temperature.
pH level : pH 1

## Slide 16
Results and discussion
Microstructure Analysis
Sample Name | Energy density (J/mm3) | Post treatment | relative density | porosity
ED20 | 21.0 | No | 93.96 % | 6.04%
ED30 | 33.3 | No | 99.48 % | 0.52%
ED40 | 41.0 | No | 98.89 % | 1.11%
ED30T | 33.3 | Yes | 99.81 % | 0.19%
W-316L | Conventional manufacturing for 316L SS - Wrought Sample | Yes | 99.68 % | 0.32%
ED:20
ED:30
ED:40
ED: 30T
Wrought 316L
Relative Density and Porosity
  Lowest energy density, highest porosity
  Umelted powder
  Grain size
  Grain shape
Figure 10 Optical micrographs of as-received samples

## Slide 17
Results and discussion
X-Ray Diffraction

## Slide 18
Results and discussion
Corrosion Behavior in room temperature NaCl
Figure 12 Cyclic potentiodynamic polarization curves at 3.5 % NaCl solution at four different pH values. A) at pH 1 B) at pH 3 C) at pH 5 and D) at pH 7.5
Figure 11 Corrosion rate of studied samples at different pH values based on CPDP Curves

## Slide 19
Results and discussion
Corrosion Behavior in room temperature NaCl
Figure 14 Corrosion rate versus Relative density extracted from Linear Polarization Resistance (LPR) results in 3.5% NaCl solution at pH 1
Figure 13 Linear Polarization Resistance (LPR) of all specimens in 3.5 % NaCl solution A) at pH 1 B) at pH 3 C) at pH 5 and D) at pH 7.5. without ED-20.

## Slide 20
Results and discussion
Corrosion Behavior in room temperature NaCl
Figure 15 SEM image for pits on a) ED20 b)ED30 c) ED40 d) ED30T e) W-316L immersed in 3.5% NaCl solution at pH 1

## Slide 21
Results and discussion
Figure 16 Typical 3D profilometer images, 2D optical images, and line profiles showing the pit density and depth for A) W316L at 3.5% NaCl, B) ED30 at 3.5% NaCl, C) W316L at crude oil, D) ED30 at crude oil.
long-duration immersed sample in Hydrocarbon and NaCl
Corrosion rate after 14 days immersion
Corrosion rate after 14 days immersion
  Immersion solution: 3.5 NaCl and crude oil
  pH : 1
  Temerature: room T
solution | Sample IDs | Calculated Corrosion rate
 |  | mpy *10^-2 (Effic.%)
3.5 NaCl, pH1 | W-316L | 7.97
 | ED30T | 4.84
Crude oil, pH 1 | W-316L | 2.66 (66.6 %)
 | ED30T | 1.56 ( 67.7 % )
Optical Profilometer

## Slide 22
Results and discussion
Figure 18 Corrosion rate versus temperature extracted from LPR results.
Pit Evaluation (pit density, pit depth and pit size)

## Slide 23
Conclusion and recommendations
  The pitting resistance of the SLM-316L stainless steel was found to be higher than that of the wrought alloy.
  In crude oil, the corrosion resistance of SLMed 316L was greater than in the 3.5% NaCl solution.
  The SLMed 316L sample has better corrosion resistance at high temperatures than wrought sample.
Conclusion:
Recommendation:
  Study the SLMed metal samples in an alkaline environment ( pH range: 7 to 14).
  More attention needs to be put on the weldability of the SLMed material and its effect on the microstructure and corrosion behavior.
Notes: Conclusion:
  The pitting resistance of the SLM-316L stainless steel was found to be higher than that of the wrought alloy, especially at pH 1, where the Epit values of the samples show a clear difference.
  In crude oil, the corrosion resistance of SLMed 316L was greater than in the 3.5% NaCl solution. This suggests that SLMed 316L could be a promising material for oil and gas pipelines and other oil ang gas industry environments.
Recommendation:
  Study the SLMed metal samples in an alkaline environment ( pH range: 7 to 14). Is it more corrosion resistant, such as in an acidic environment, or will the trend change?
  More attention needs to be put on the weldability of the SLMed material and its effect on the microstructure and corrosion behavior.
  Study 3 D printed materials in high temperature hydrocarbon environment.

## Slide 24
References
H. M. Hamza, K. M. Deen, A. Khaliq, E. Asselin, and W. Haider, “Microstructural, corrosion and mechanical properties of additively manufactured alloys: a review,” Critical Reviews in Solid State and Materials Sciences, vol. 47, no. 1. Taylor and Francis Ltd., pp. 46–98, 2022. doi: 10.1080/10408436.2021.1886044.
A. Concilio and L. Lecce, Shape Memory Alloy Engineering: For Aerospace, Structural and Biomedical Applications. 2014. doi: 10.1016/C2012-0-07151-7.
by Albert E. Patterson,Sherri L. Messimer and Phillip A. Farrington “Overhanging Features and the SLM/DMLS Residual Stresses Problem: Review and Future Research Need”. https://www.mdpi.com/2227-7080/5/2/15.
B. A. AlMangour, “Additive manufacturing of high-performance 316L stainless steel nanocomposites via selective laser melting,” University of California, Los Angeles, no. 2017.
Q. Chao et al., “On the enhanced corrosion resistance of a selective laser melted austenitic stainless steel,” Scr Mater, vol. 141, 2017, doi: 10.1016/j.scriptamat.2017.07.037.
G. B. Bang et al., “Effect of process parameters for selective laser melting with SUS316L on mechanical and microstructural properties with variation in chemical composition,” Mater Des, vol. 197, Jan. 2021, doi: 10.1016/j.matdes.2020.109221.
H. Maicas-Esteve, I. Taji, M. Wilms, Y. Gonzalez-Garcia, and R. Johnsen, “Corrosion and Microstructural Investigation on Additively Manufactured 316L Stainless Steel: Experimental and Statistical Approach,” Materials, vol. 15, no. 4, Feb. 2022, doi: 10.3390/ma15041605.

## Slide 25
Reach out.
THANK YOU
Q&A
email
phone
Calle Cualquiera 123, Cualquier Lugar
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES
YOUR LOGO
0553786980
Ibrahim.a.albalawi@gmail.com

## Slide 26
Appendix
Calle Cualquiera 123, Cualquier Lugar
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES
YOUR LOGO

## Slide 27
T | Sample IDs | Icorr µA | Ecorr mV | CR mpy | Rp kΩ.cm2 | Eff %
25 C | W-316L | 0.10 | -158.17 | 0.044 | 308.625 | 
 | ED30T | 0.06 | -102.85 | 0.028 | 420.65 | 35%
70 C | W-316L | 7.407 | -304.05 | 3.3845 | 3.5665 | 
 | ED30T | 0.005 | -290.05 | 2.127 | 5.6015 | 99.9%
Polarization resistance (Rp), corrosion current density (Icorr), and corrosion rate obtained from Linear Polarization Resistance (LPR) plots in 3.5 % NaCl solution at pH 1 room and 70 C temperature
Figure 18 Linear Polarization Resistance (LPR) plots of SLMed 316L and wrought 316L samples in 3.5 % NaCl at room temperature and 70 C
Figure 18 Corrosion rate versus temperature extracted from LPR results.
Corrosion Behavior at High Temperature NaCl
Figure 19 Cyclic potentiodynamic polarization curves at 3.5 % NaCl solution

## Slide 28
Thickness of passive layer |  |  |  |  |  |  | 
pH | Sample IDs |  |  |  |  |  | 
 |  | e | e0 | A | Cf | Lss | Deta
1 | W-316L | 15.6 | 8.85E-14 | 0.7854 | 6.51E-05 | 1.67E-08 | 
 | ED20 | 15.6 | 8.85E-14 | 0.7854 | 4.34E-04 | 2.50E-09 | -1.42E-08
 | ED30 | 15.6 | 8.85E-14 | 0.7854 | 7.02E-05 | 1.55E-08 | -1.21E-09
 | ED30T | 15.6 | 8.85E-14 | 0.7854 | 5.57E-05 | 1.95E-08 | 2.81E-09
 | ED40 | 15.6 | 8.85E-14 | 0.7854 | 6.45E-05 | 1.68E-08 | 1.55E-10
3 | W-316L | 15.6 | 8.85E-14 | 0.7854 | 7.02E-05 | 1.55E-08 | 
 | ED20 | 15.6 | 8.85E-14 | 0.7854 | 7.55E-04 | 1.44E-09 | -1.40E-08
 | ED30 | 15.6 | 8.85E-14 | 0.7854 | 7.32E-05 | 1.48E-08 | -6.33E-10
 | ED30T | 15.6 | 8.85E-14 | 0.7854 | 5.30E-05 | 2.05E-08 | 5.02E-09
 | ED40 | 15.6 | 8.85E-14 | 0.7854 | 7.55E-05 | 1.44E-08 | -1.08E-09
5 | W-316L | 15.6 | 8.85E-14 | 0.7854 | 5.38E-05 | 2.02E-08 | 
 | ED20 | 15.6 | 8.85E-14 | 0.7854 | 2.09E-04 | 5.19E-09 | -1.50E-08
 | ED30 | 15.6 | 8.85E-14 | 0.7854 | 5.33E-05 | 2.04E-08 | 1.89E-10
 | ED30T | 15.6 | 8.85E-14 | 0.7854 | 3.57E-05 | 3.04E-08 | 1.02E-08
 | ED40 | 15.6 | 8.85E-14 | 0.7854 | 5.12E-05 | 2.12E-08 | 1.02E-09
7.5 | W-316L | 15.6 | 8.85E-14 | 0.7854 | 3.28E-05 | 3.31E-08 | 
 | ED20 | 15.6 | 8.85E-14 | 0.7854 | 8.81E-04 | 1.23E-09 | -3.18E-08
 | ED30 | 15.6 | 8.85E-14 | 0.7854 | 4.79E-05 | 2.26E-08 | -1.04E-08
 | ED30T | 15.6 | 8.85E-14 | 0.7854 | 3.22E-05 | 3.37E-08 | 6.16E-10
 | ED40 | 15.6 | 8.85E-14 | 0.7854 | 3.90E-05 | 2.78E-08 | -5.26E-09
Electrochemical impedance spectroscopy (EIS) , Bode plots of all specimens in 3.5 % NaCl solution A) at pH 1 B) at pH 3 C) at pH 5 and D) at pH 7.5.
The steady-state film thickness (Lss)
Corrosion Behavior in room temperature NaCl

## Slide 29
Corrosion Behavior in room temperature NaCl
Figure 14 Cyclic potentiodynamic polarization curves at 3.5 % NaCl solution at four different pH values. A) at pH 1 B) at pH 3 C) at pH 5 and D) at pH 7.5
Figure 13 Corrosion rate of studied samples at different pH values based on CPDP Curves
pH | Sample IDs | W-316L | ED20 | ED30 | ED30T | ED40
1 | CR (mpy) | 2.78 | 17.58 | 7.75 | 1.75 | 3.60
 | Eff % |  | -533.98% | -179.63% | 36.78% | -29.82%
3 | CR (mpy) | 1.55 | 11.08 | 1.02 | 0.14 | 0.67
 | Eff % |  | -617.24% | -2.32% | 93.63% | -57.47%
5 | CR (mpy) | 0.21 | 6.08 | 0.23 | 0.17 | 0.18
 | Eff % |  | -188.05% | -11.39% | 20.26% | 17.05%
7.5 | CR (mpy) | 0.11 | 5.63 | 0.17 | 0.07 | 0.14
 | Eff % |  | -248.99% | -57.19% | 38.08% | -32.14%

## Slide 30
The results of Tafel fitting extract from CPDP curve at pH1, pH3, pH5, and pH7.5 solution
pH | Sample IDs | Beta A mV/dec | Beta C mV/dec | Icorr µA/cm2 | Ecorr mV | CR mpy | Eff % | Ipit µA | Epit mV | Erep mV | Epit-Erep | 
1 | W-316L | 7.5E+14 | 0.08 | 2.13 | -307.0 | 2.78 | - | 3.35 | 423.10 | 71.43 | 351.6 | 
 | ED20 | 5.3E-01 | 0.17 | 13.5 | -322.0 | 17.5 | -533% | 236.5 | 115.4 | -208.8 | 324.2 | 
1 | ED30 | 1.0E+15 | 0.11 | 5.95 | -343.0 | 7.75 | -179% | 3.57 | 439.60 | 5.49 | 434.11 | 
 | ED30T | 4.0E+14 | 0.22 | 1.35 | -248.6 | 1.75 | 36% | 3.93 | 494.50 | 60.95 | 433.55 | 
 | ED40 | 3.3E+14 | 0.10 | 2.76 | -271.0 | 3.60 | -29% | 746.40 | 285.70 | 93.40 | 192.30 | 
3 | W-316L | 4.0E+14 | 0.11 | 1.19 | -461.00 | 1.55 |  | 2.70 | 340.7 | 170.3 | 170.40
 | ED20 | 5.85E-01 | 0.50 | 8.53 | -326.00 | 11.08 | -617% | 198.5 | 263.7 | -186.8 | 450.50
 | ED30 | 1.0E+15 | 0.09 | 1.22 | -474.00 | 1.02 | -2.3% | 3.74 | 615.40 | -5.35 | 620.75
 | ED30T | 8.15E-01 | 2.E+14 | 0.08 | -457.53 | 0.14 | 93% | 3.74 | 653.20 | 10.99 | 642.21
 | ED40 | 5.0E+14 | 0.05 | 1.87 | -238.12 | 0.67 | -57% | 4.60 | 696.40 | 43.96 | 652.44

## Slide 31
The results of Tafel fitting extract from CPDP curve at pH1, pH3, pH5, and pH7.5 solution
5 | W-316L | 3.67E-01 | 0.16 | 0.16 | -174.60 | 0.21 |  | 4.97 | 554.90 | 104.40 | 450.50
 | ED20 | 5.12E-01 | 0.27 | 0.47 | -129.00 | 6.08 | -188% | 128.80 | 329.70 | 126.20 | 203.50
 | ED30 | 1.35E+00 | 0.14 | 0.18 | -304.00 | 0.23 | -11% | 3.46 | 653.80 | -104.0 | 758.20
 | ED30T | 2.00E+14 | 0.22 | 0.13 | -210.00 | 0.17 | 20% | 4.04 | 604.00 | 120.90 | 483.10
 | ED40 | 1.96E+00 | 0.14 | 0.13 | -244.00 | 0.18 | 17% | 6.69 | 806.30 | -10.99 | 817.29
7.5 | W-316L | 5.94E-01 | 0.09 | 0.08 | -187.60 | 0.11 |  | 3.10 | 489.00 | -10.49 | 499.49
 | ED20 | 6.29E-01 | 0.26 | 0.29 | -174.00 | 5.63 | -248% | 71.50 | 258.20 | -169.30 | 427.50
 | ED30 | 7.57E-01 | 0.10 | 0.13 | -319.00 | 0.17 | -57% | 5.02 | 659.30 | -142.90 | 802.20
 | ED30T | 4.49E-01 | 0.09 | 0.05 | -191.40 | 0.07 | 38.% | 5.40 | 604.40 | 6.42 | 597.98
 | ED40 | 3.76E-01 | 0.11 | 0.11 | -228.00 | 0.14 | -32% | 5.20 | 833.40 | -4.60 | 838.00
pH | Sample IDs | Beta A mV/dec | Beta C mV/dec | Icorr µA/cm2 | Ecorr mV | CR mpy | Eff % | Ipit µA | Epit mV | Erep mV | Epit-Erep

## Slide 32
Corrosion Behavior in room temperature NaCl
EDS results for W-316L pit
EDS results for ED 30T pit

## Slide 33
Linear Polarization Resistance (LPR) of all specimens in 3.5 % NaCl solution A) at pH 1 B) at pH 3 C) at pH 5 and D) at pH 7.5.

## Slide 34
Section 4.1 and 4.2
Material and fabrication
Section 4.3
Density measurement
Section 4.4
Microstructure characterization
Section 4.5
Corrosion test
Section 4.6
Immersion test

## Slide 35
The process for the formation of water-in-oil emulsions