## Slide 1
Analytical Techniques Essential for corrosion studies
Arun Kumar.S, Mohammad T. Akhtar, Ahmad Khudir Al-Raddadi,Nasheri-Al, Mansour Mohammad,
Ahmad Al-Musharaf
Presented By: Arun Kumar. S
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES

## Slide 2
Outline

## Slide 3
Industrial process are controlled – Analytical results are the indicator of controllability

## Slide 4
Background
Most of the Refinery and petroleum process corrosion sample are contaminated and at
  Correlation
  Resolve
  Plan
Sampling
  Representative samples
  Relation to DP
  Turnaround
  Fouling
  Deposits – different section
  Limited samples ( low volume/weight)
Figure 1: Different type of sample collection for corrosion studies
Corrosion initiation
  Fouling, acidic, basic, halides
  Pitting, Erosion
  Leaks and failure.
Analytical Challenges.
  Undesired condition
  Testing protocol

## Slide 5
Problem description & objectives
Quick screening :XRF, XRD, SEM EDX
  % level
  Challenges – Nature of sample
      Aqueous / organic.
      Low volume & low concentration
      Organic components
KSA is also hub
  PVC and chlorine related products
  Correlate -industry and corrosion studies using certified standard
Surface effect and corrosion residue using different analytical technique.
Exploring other Analytical for limited or corrosive samples
Figure 2: Solution obtained by treating CS and Austenitic steel samples

## Slide 6
Methodology
Methodology
Experimental setup
Optical Microscopy
Energy dispersive spectroscopy (EDS)
ICP-MS, IC, Gas Chromatography
Scanning Electron Microscope (SEM)

## Slide 7
Results & Discussion

## Slide 8
The higher scaling is observed for the Carbon steel in all three acidic solution.
The color ranges between dark brown and reddish orange
Majority of the residue is Hematite in Carbon Steel sample
Pronounced attack of A.Alloy is observed in Hydrochloric acid.
A mild attack of Acetic acid in A.Alloy compared to Carbon steel
Two Alloys were chosen for experiments with three chemicals : HCL , HNO3 & Acetic Acid
  Carbon Steel
  Austenitic Steel
  Conditions
    Room Temperature
    HCl (35%), HNO3 (65%) & Acetic Acid (10%)
    Time 2 Days
  Experimental setup
Table 1: Elemental composition of the carbon & Austenic steel
Results & Discussion
Elemental composition of Austenitic steel-13x 17001 |  |  |  |  | 
C | Si | S | P | Mn | Ni
0.114 | 0.34 | 0.016 | 0.08 | 1.73 | 6.05
Cr | Mo | Cu | Co | Al | Nb
14.89 | 0.12 | 0.037 | 0.15 | 0.01 | 0.76
Elemental composition of Carbon Steel -3952 |  |  |  |  | 
C | Si | S | P | Mn | Ni
0.114 | 0.34 | 0.002 | 0.001 | 0.5 | 0.112
Cr | Mo | Cu | Co | Al | Nb
0.105 | 0.519 | 0.202 | 0 | 0.048 | 0.76
Figure 3: Images of CS and Austenic steel after chemical treatment
A.Alloy Steel
A. Alloy Steel- HNO3
A.Alloy Steel- HCl
A. Alloy Steel- AA
C Steel
C Steel- HNO3
C Steel- HCl
C Steel- AA

## Slide 9
  SEM Analysis
Results & Discussion
Spectrum | A2 | A4
O | 26.79 | 0
Cl | 0.93 | 
Cr | 28.38 | 16.89
Fe | 31.73 | 71.32
Ni | 1.84 | 8.36
Nb | 0.28 | 0.63
Spectrum | A3 | A4
Cl |  | 0.2
O |  | 30.05
Si | 0.18 | 0.21
Ca |  | 0.42
Fe | 96.33 | 42.5
Mo | 0.46 | 0.31
Extract of metals with different Acid
Optical images for CS in HCl
Optical images for A.A in HCl
Sample solution analyzed by ICP-MS
Sample solution analyzed by ICP-MS
EDS analysis –Depletion in Metals.
As SEM-EDX optical technique limitation
Solution-Acidic/Organic
ICPMS Analysis
ICP/ ICPMS technique
Minimum samples volume
    0.5ml
    Digesting -Clear solution
    A. Alloys pronounced
    CS Steel oxidized in HNO3 – Iron oxide

## Slide 10
  Chromatography
Results & Discussion
Figure 7 high chloride content even after washing the residue with water
Figure 5: Ion chromatography analysis of the organic acid
Figure 6 GC-MS Mass spectrum organic Acid and Sulfur species
Ion chromatography -corrosion initiators
low as 0.5mL sample volume.
GC-MS chromatography -Unknow volatile impurities
  Anions
  Organic Acid
  Trace Sulfur species – Thio compounds
  Organic Chloride

## Slide 11
Conclusions

## Slide 12
Analytical Techniques have several advantages and some limitation.
During sampling the extent of care taken would determine the effective analysis and the correlation.
Sample as low as 0.001g/ 0.1ml quantity which are deposited/ adhering to surface can provide useful information.
ICP/ ICP-MS as an alternative tool in absence of XRF or EDX , can provide information to level of low concentration.
Trace corrosion initiators like organic Sulfur, Chloride, Amines… can be identified and quantified.
Combustion Ion chromatography can add advantage in quantification of Trace halides for several type of samples which can be an alternative.
  Conclusions
Conclusions & Recommendations

## Slide 13
References
[1] Georgios Fytianos, rrosion evaluation of MEA solutions by SEM-EDS, ICP-MS and XRD, Energy Procedia 86 ( 2016 ) 197 – 204
[2] Ionita, Daniela, CP-MS determinations in sustaining corrosion data of 316 stainless steels in bioliquids, UPB Scientific Bulletin, Series B: Chemistry and Materials Science, I 2014/01/01.
[3] Vincent Souchon, Marc Maleval, Fabien Chainet, Charles-Philippe Lienemann. Chlorine speciation in complex hydrocarbon matrices using GC-ICP-MS/MS. Journal of Analytical Atomic Spectrometry, 2023, 38 (8), pp.1634-1642. ff10.1039/d3ja00066dff. ffhal-04289902

## Slide 14
Reach out.
THANK YOU
rajua@sabic.com
+966 13 359 9170
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES