## Slide 1
Jubcor Presentation
King Fahd University of Petroleum and Minerals
Presented By: Abdulaziz Alsaleh & Dr. Ihsan Ul haq Toor
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES

## Slide 2
Hydrogen Economy
Hydrogen Economy
Demand of Energy in different industries over the year

## Slide 3
Saudi Arabia & Hydrogen
Current and projected hydrogen production costs in Saudi Arabia

## Slide 4
What is Embrittlement?
Embrittlement, where materials become brittle from reduced ductility, which leads to cracking or failure.
Types of Embrittlement
Hydrogen embrittlement, 3. Temper embrittlement
2. Liquid metal embrittlement, 4. Sulfide Stress Cracking (SSC)
Hydrogen molecules diffuse through metals and create pressure inside the cavities
Hydrogen molecules accumulate and create pressure and cause carking

## Slide 5
Stages of Embrittlement
H-Ion generation
Adsorption
Absorption
Diffusion
Trapping
Cracking

## Slide 6
Experiment Scenario
Sample Number | Heat Treatment Temperature (°C) | Hydrogen Charging Duration (hours)
1 | 550 | 12
2 |  | 24
3 |  | No Exposure
4 | 600 | 12
5 |  | 24
6 |  | No Exposure
7 | 650 | 12
8 |  | 24
9 |  | No Exposure
10 | As-Received | 12
11 |  | 24
12 |  | No Exposure

## Slide 7
Methodology
Solution: H2SO4
NH4SCN
H2O
Heat Treatment
550, 600 & 650oC
Hydrogen Charging
Impact Testing
Fractography
Room Temperature
Atmospheric Pressure
Elements | C | Mn | Si | Ti | P | S | V | Nb | Fe
Chemical Composition (%Mass) | 0.16 | 1.65 | 0.45 | 0.06 | 0.02 | 0.01 | 0.07 | 0.05 | ~97.53
Table 1, X65 API 5L Chemical Composition

## Slide 8
Sample Preparation
The standard Charpy impact test specimen is of dimension 55 mm × 10 mm × 10 mm
Exposed Area of specimen 36.5 mm × 10 mm × 10 mm
Exposed Area
Insulated by Tape
x 4 = 14.60 A

## Slide 9
Solution Preparation
Hydrogen Cathodic Charging Solution Contains:
Component | Concentration | Volume Added
Sulfuric Acid (H2SO4) | 0.2 M | 10.93 mL
Ammonium Thiocyanate (NH4SCN) | 3 g/L | Calculated to make 1 L
H2O | - | 899 mL
Sulfuric Acid:
  Density of H₂SO₄: 1860 g/cm³.
  Mass of H₂SO₄ in Stock Solution:0.966×1860=1796.76 g/L
  Molar Mass of H₂SO₄: 98 g/mol.
  1796.76 g/L x 98 g/mol=18.3
  𝐶1 x 𝑉1=𝐶2 x 𝑉2 ⟹ 18.3×𝑉1=0.2×1000 ⟹ 𝑉1=10.93 mL

## Slide 10
Results & Discussion
Effect of Hydrogen Charging and heat Treatment on the Impact Energy of X65 alloy
Hydrogen charging decreased the impact energy of X65 alloy irrespective of the heat treatment temperature.
Heat Treatment was effective in reducing the impact of hydrogen charging on X65 alloy.
Stress releasing heat treatment at 550oC produce the best performance to mitigate the effect of hydrogen charging.
The impact energy of X65 alloy was not affected by heat treatment when not subjected to hydrogen charging.
The fracture surface is characterized with the presence of micro cracks and dimples

## Slide 11
Fractography
Micro cracks
dimples
As - Received
Heat Treated 650

## Slide 12
References
Hydrogen: A Renewable Energy Perspective. September 2019. Report prepared for the 2nd Hydrogen Energy Ministerial Meeting, Tokyo, Japan.
Take Early Action to Avoid Hydrogen Embrittlement. MagnaPlate Blog. Available at: magnaplate.com. This blog discusses preventive measures against hydrogen embrittlement in materials.
Hasan, S., & Shabaneh, R. (2021). The Economics and Resource Potential of Hydrogen Production in Saudi Arabia. DOI: 10.30573/KS--2021-DP24. November 2021. This study discusses the economic viability and resource potential of hydrogen production in Saudi Arabia.
Department of Energy. (2024). Hydrogen Program Plan. U.S. Department of Energy. Retrieved from https://www.energy.gov/hydrogen-program-plan

## Slide 13
Acknowledgment
Acknowledgement: The authors acknowledge the support provided by King Fahd University of Petroleum and Minerals (KFUPM),Dhahran, Saudi Arabia, under the research grant# INAM 2406 for conducting this research work.

## Slide 14
Reach out.
THANK YOU
Azizalsaleh-98@hotmail.com
+966508092568
Calle Cualquiera 123, Cualquier Lugar
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES
YOUR LOGO