## Slide 1
Jubcor Presentation
Flexible Passive Fire Protection
Mohmmed Alnasser
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES

## Slide 2
Hydrocarbon Fire
Cellulosic Fire
PASSIVE FIRE PROTECTION SOLUTIONS INCLUDE:
Passive fire protection Material (PFP) is crucial for preventing or delaying the spread of fire, thereby providing crucial time for evacuation and minimizing damage to property.
WHAT IS PFP

## Slide 3
Type of Fireproofing | Cementitious Fireproofing | Waterborne Fireproofing | Solvent Based Fireproofing | Epoxy based Fireproofing
Appearance | Rough | Smooth | Smooth | Smooth
Application | Spray | Spray | Spray | Spray
Fire Resistance | Up to 3 Hrs | Up to 2 Hrs | Up to 3 Hrs | Up to 3 Hrs
Durability |  |  |  | 
Maintenance | Regular | No | No | No
Weight |  |  |  | 
Environment | Up to C5 | Up to C3 | Up to C5 | Up to C5
Flexibility |  |  |  | 
Corrosion Protection |  |  |  | 

## Slide 4
Meet AESS* Finish Standard No. 3: Feature Elements in Close View – High decorative finish without sanding
Smooth surface after cured
Good appearance even without topcoat
Less weight, allowing lower transportation cost
No smoothing putty required
Approx. 20% labor/ cost saving
Cleaner, more durable aesthetic
Other PFP
Typical cementitious fire protection
*Architecturally Exposed Structural Steel
by The American Institute of Steel Construction (AISC)
Cementitious Vs. Other PFP

## Slide 5
Provides good flexibility at harsh environment
No cracking after 30 cycles during cycle test vs. competitor (IP Interchar 212) cracked after 15 cycles
No cracking before 10.5mm displacement even at -40ºC vs. competitor (Jotun Steelmaster 1200HPE 5.0mm)
Benefits
Less damage during handling and transportation
Wider tolerance for application environment (especially at low temperature)
Save time & labor cost for repair
Flexibility
3-Point Bending Test

## Slide 6
Designed for in-shop and on-site application by dry trowel, single or plural component airless spray.
6
Key features – Application benefits
Unrivalled in its outstandingly smooth, architectural finish.
More aesthetic option than
traditional cementitious products.
Up to 3500 µm DFT in a single coat, cures rapidly for a quick and efficient building process.
On-site / off-site application
Applied within 1 day / transferred to the site next day
Smooth and flexible finish

## Slide 7
7
Best in class thicknesses in some ranges
Less conflicts on-site
Flexible surface providing excellent damage resistance
Highly competitive thicknesses, gives cost effective protection built with lower material and labour investment.
Reduced works on site, working at height, which also improves safety.
Flexible surface providing excellent damage resistance, easy for safe construction and transportation.
Key features – Application benefits

## Slide 8
Best in class thicknesses in some ranges
Less conflicts on-site
Flexible surface providing excellent damage resistance
Highly competitive thicknesses, gives cost effective protection built with lower material and labour investment.
Reduced works on site, working at height, which also improves safety.
Flexible surface providing excellent damage resistance, easy for safe construction and transportation.
Key features – Benefits for applicators and installers

## Slide 9
Reach out.
THANK YOU
email
phone
JUBCOR
CONFERENCE & EXHIBITION
2024
INNOVATIVE SOLUTIONS FOR CORROSION CHALLENGES